## Slide 1: Multicore fibres and photonic lantern
University of Bath, UK
6 November 2014
Itandehui Gris-Sánchez

## Slide 2
Photonics for planets

## Slide 3
What is an optical fibre?
Optical waveguide made out of a dielectric material most commonly high purity silica glass, usually several km long.
Typical low loss window:
800 nm to 1600 nm.
Photonics for planets

## Slide 4
How does an optical fibre guide light?
http://drhart.ucoz.com/Research/fiber_modes.png
  Huygens-Fresnel principle
  Geometric optics?
Photonics for planets
Notes: What is a mode?
  Stationary solution of the envelope of the field. Result from the interference of the wavelets reflected inside the fibre

## Slide 5: Standard vs Specialty
Photonics for planets
Notes: Optical fibres as commonly know are widely used in telecom industry. The understanding of the physical guiding mechanisms is clear and the fabrication is cheap and fibre now have high performance telecommunications. Changes in the geometry design and in the materials effectively change guiding mechanisms

## Slide 6
Previous work:
Multicore fibre terminated with lanterns
Photonics for planets
TA Birks et al, Opt Express 20 (2012) 13996

## Slide 7
Step-index MMF
input
mode scrambler:
step-index MMF
Photonics for planets
TA Birks et al, Opt Express 20 (2012) 13996

## Slide 8
TA Birks et al, Opt Express 20 (2012) 13996
Lantern-terminated MCF
input
MCF with lanterns
mode scrambler:
step-index MMF
Photonics for planets

## Slide 9
TA Birks et al, Opt Express 20 (2012) 13996
Lantern-terminated MCF
input
step-index MMF
MCF with lanterns
t = 0.1 s
mode scrambler:
Photonics for planets
Notes: MCF (121 identical cores) act as a mode scrambler

## Slide 10
73x7 (511 cores 1.77 to 3.34um
Multicore fibre scrambler
Photonics for planets
V=2.4 @ =860 nm
V=5.4 @ =380 nm
N=
N=480
Notes: Multicore fibre as a relay with fixed FRD and modal noise scrambling (giving incoherent output intensity distribution independent of the input intensity distribution or position i.e. a range of higher order modes) minimal bend loss compared to large core low NA fibres
DM Haynes et al, SPIE (2014) 915155

## Slide 11
Photonics for planets
~ 310um
~ 55 um
~ 1 mm
~ 560 um
V<0.5um

## Slide 12: What is a photonic lantern?
1 MM core with N modes
low-loss interface between multimode and single-mode waveguides:
N  SM cores
mode-number matching:
MM modes = SM cores
output distribution of light is unimportant
SG Leon-Saval et al, Opt Lett 30 (2005) 2545
Photonics for planets

## Slide 13: Reciprocal device
low-loss interface between single-mode and multimode waveguides:
N SM cores
1 MM core with N modes
SG Leon-Saval et al, Opt Lett 30 (2005) 2545
mode-number matching:
MM modes = SM cores
output distribution of light is unimportant
Photonics for planets

## Slide 14: Taper transition
TA Birks et al, Opt Express 20 (2012) 13996
mode 42
mode 42
mode of MM core
supermode of coupled SM cores
independent SM cores
 adiabatic 
Photonics for planets

## Slide 15: Propagation between two lanterns
mode of MM core
supermode of coupled SM cores
independent SM cores
phases preserved
same supermode
same mode
identical paths
ideal case:
Photonics for planets

## Slide 16: Propagation between two lanterns
mode of MM core
supermode of coupled SM cores
independent SM cores
phases scrambled
several supermodes
severalmodes
perturbed paths
mode spectrum: scrambled, uniformly filled, insensitive to input
losses: MM transmission line with SM performance
mode-number matching
realistic case:
TA Birks et al, Opt Express 20 (2012) 13996
N=
Photonics for planets
Notes:   Fixed FRD

## Slide 17: Photonic lanterns, Type 1
SMFs tapered in a photonic crystal fibre template
SG Leon-Saval et al, Opt Lett 30 (2005) 2545
19 SMFs
~4 mm
145 µm
MMF
19 SMF
MMF
transition
Photonics for planets

## Slide 18: Photonic lanterns, Type 2
SMFs tapered in a low-index glass capillary
D Noordegraaf et al, Opt Express 17 (2009) 1988
D Noordegraaf et al, Opt Express 18 (2010) 4673
N = 61 SMFs
0.76 dB loss
NK Fontaine, OFC (2013) OTh1B.3
DB Mortimore et al, Appl Opt 30 (1991) 650
Photonics for planets

## Slide 19: Photonic lanterns, Type 3
multicore fibre tapered in a low-index glass capillary
oxy-butane flame
F-doped silica capillary
MCF
TA Birks et al, Opt Express 20 (2012) 13996
loss < 0.5 dB
Photonics for planets

## Slide 20: Photonic lanterns, Type 4
integrated optics, eg ultrafast laser inscription
RR Thomson et al, Opt Express 19 (2011) 5698
I Spaleniak et al, Opt Lett 21 (2013) 27197
Photonics for planets

## Slide 21: Tapering the jacketed MCF
TA Birks et al, JLT 10 (1992) 432
fibre
oxy-butane burner
Photonics for planets

## Slide 22: Some remarks
MCF terminated with photonics lanterns act as low FRD relay with broadband operation with incoherent output intensity distribution
Potential in MM and SM interfaces:
  Mode scrambler
  MM spectral filtering
Photonic lantern: conversion between a multimode port and a multiport system
4 existing lantern technologies
Photonics for planets

## Slide 23: Spare slides
Photonics for planets

## Slide 24: Adjusting the geometry
SG Leon-Saval et al, Nanophotonics 2 (2013) 429
are they the right N modes?
MM core
good array geometry
bad array geometry
NK Fontaine et al, Opt Express 20 (2012) 27123
Photonics for planets

## Slide 25
Diameter monitor
Preform feed
Furnace
Coating cup
UV lamp
Vfeed
Vdraw
Capstan
Take-up
Hot zone
Vacuum and pressure lines
Photonics for planets
Notes: Mention the parts names

## Slide 26: PCF and multicore fibre fabrication
Stack and draw
Photonics for planets